## Slide 1: Surface Plasmon Polaritons – Light confined to 2D
Why confine light to 2D?
What are SPPs?
What can support SPPs?
How can you excite SPPs?
Neat things you can do with SPPs

## Slide 2: Why confine light?
J. Phys. Chem. C, 2015, 119 (17), pp 9506–9512
Siu et al, Nanophotonics, 3 125 (2014)
IEEE Photonics Journal ( Volume: 5, Issue: 4, Aug. 2013 )
SPP-enhanced photochemistry
Integrated Optical Circuits for computing
SERS with SPPs

## Slide 3: What is an SPP?
Surface Plasmon Polariton: Light guided along a metal surface

## Slide 4: Light confined to Two Dimensions
SPPs propagation and attenuation related to effective indices

## Slide 5: Light confined to Two Dimensions
SPPs propagation and attenuation related to effective indices

## Slide 6: Predicted ~1957 by Rufus Ritchie Proposed that SPPs could be excited by firing energetic electrons at thin metal films

## Slide 7: SPP Dispersion
Plasmonic Fingerprints
Total energy of photon or electron used to excite SPP
Momentum parallel to surface proportional to this:

## Slide 8: Let’s Calculate our own SPP fingerprints!

## Slide 9: Let’s Calculate our own SPP fingerprints!

## Slide 10: Let’s Calculate our own SPP fingerprints!
Which are SPPs and which are not?

## Slide 11: How to excite SPPs?
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 12
What is momentum of the SPP proportional to?
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 13
What is momentum of the SPP proportional to?
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 14
What is momentum of the SPP proportional to?
What is momentum of the laser beam above proportional to?
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 15
What is momentum of the SPP proportional to?
What is momentum of the laser beam above proportional to?
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 16
Momentum Matching Condition:
or
The key is to match energy & momentum of your excitation source to the energy & momentum of the SPP

## Slide 17: How do you excite SPPs?
Many people have claimed that you excite SPPs precisely at the angle at which reflection from the metal film is minimized. Many people have been wrong!

## Slide 18: How do you excite SPPs?
k0 (μm-1)
Amplitude
β (μm-1)
θ (deg.)
a)
c)
514 nm
Amplitude
θ (deg.)
Two finger prints can be found: One follows minimum reflectance angle, one follows maximum transmission amplitude angle
doi:10.1038/srep09929

## Slide 19: What’s excited at the Kretschmann-Raether minimum? A Perfectly Absorbing Mode!
PA Mode
SPP Mode

## Slide 20
Excitation at angle that gives max in transmission amplitude
1
0
-1
Driven at 44.9°
Propagating
z
x
β = 13.11
FDTD
β = 13.14
FDTD
Re(Ex)
Distance (nm)
Distance (nm)
Re(Ex)

## Slide 21
-1
1
0
-1
Driven at 54.2°
Propagating
z
x
β = 14.76
FDTD
β = 13.43
FDTD
Re(Ex)
Re(Ex)
Distance (nm)
Distance (nm)
Excitation at angle that gives min in Reflectance

## Slide 22
a) Kretschmann-Raether Setup
b) Leakage Radiation Setup
z
x
Experimental configurations for measuring the signatures of the SPP mode and the new mode (Perfectly absorbing mode)

## Slide 23
SPR and/or PA Resonance can be used to measure thermodynamic and kinetic properties ligand binding
Gibbs Free Energy under standard conditions related to equilibrium constant:
Observable signal when

## Slide 24
SPR and/or PA Resonance can be used to measure thermodynamic and kinetic properties ligand binding
Gibbs Free Energy under standard conditions related to equilibrium constant:
Observable signal when

## Slide 25
Binding events at the surface monotonically increase
Angle that gives observable signal increases as more molecules bind
Gibbs Free Energy under standard conditions related to equilibrium constant:
Observable signal when

## Slide 26
Squeezing Light down to 1-dimension
Scientific Achievement
Identified a new type of plasmon called an ISPP that results from refraction of SPPs
Significance and Impact
ISPPs provide new ways control optical energy at the nanoscale
Light guided along one metal (silver) encounters a different metal (gold), creating an ISPP
Profile of ISPP wave
Foley et al. ACS Photonics 1 739 (2014)

## Slide 27: Light confined to One Dimension?
Foley et al. ACS Photonics, 2014, 1, 739
Ag
Al
Real and Imaginary components of SPP wavevector have different refraction angles

## Slide 28: Light confined to One Dimension?
Inhomogeneous waves: real and imaginary wavevector components point in different directions

## Slide 29: Generalization of Snell’s law for SPPs?
k2’’
’
Creating inhomogeneous SPPs follows from complex Snell’s Law
Foley et al., ACS Photonics, 1, 739 (2014)

## Slide 30: Generalization of Snell’s law for SPPs?
k2’’
’
Foley et al., ACS Photonics, 1, 739 (2014)
Properties of the ISPP depend on properties of BOTH surfaces